## Slide 1
Wolfgang Rau
Queen’s University Kingston
Motivation
Experimental Setup – Diffusion Model
Measurement – Efficiency Simulation
Data Analysis
Motivation
  PE used as shielding in DM experiments
  Rn daughter 210Po may produce neutrons (,n)
  Determine allowed exposure of PE to air
Experimental Setup – Diffusion Model
Measurement – Efficiency Simulation
Data Analysis
Radon Diffusion In Polyethylene

## Slide 2
Radon Chamber
PE sample
(stack of
sheets)
Fill radon into chamber repeatedly
Let it diffuse and decay
1 Exposure - Diffusion
Constant Rn concentration
infinite exposure time  exponential profile
Actual Rn concentration C(t) (example):
 need a diffusion and decay model
x
t
t
x

## Slide 3
PE
2 Detection
 Detector
Monte Carlo for  emission (geometry)
Determine  energy loss in PE (SRIM)  detection efficiency and E spectrum
Rn decay in air pockets  surface Po
 ignore high energy events
 detector: Ortec, NIM module with two detector chambers MCA, Maestro

## Slide 4
3 Analysis
NOTE: 210Po continues to build up long after exposure (part of diff & decay model)
Fit model with 2 free parameters (diffusion constant and solubility) to data
For visualization: extrapolate and convert measured Po rate to 210Pb rate at end of exposure based on best fit model parameters
Calculated 2 contours to determine uncertainties  two parameters correlated
Calculate 210Po activity  uncertainty surprisingly small

## Slide 5
4 Short-lived Daughters
Expose single sheet
Measure immediately after end of exposure
Modeled s from 222Rn, 218Po and 214Po
3 parameters: diff. constant, surface activity, t (end of exposure – start of measurement)
NO solubility
Evaluate in 4 energy bins
Good agreement between model and data
Diffusion constant significantly larger

## Slide 6
5 Results
 | 210Po |  |  | Short-lived | 
 | Solubility | Diff const [e12 m2/s] | Diff length [mm] | Diff const [e12 m2/s] | Diff length [mm]
UHMWPE | 0.68  0.10 | 1.2  0.2 | 0.76  0.06 | 6.0  0.8 | 1.7  0.1
PE | 0.45  0.07 | 3.7 +1.4-1.0 | 1.3  0.20 | 7.1  0.8 | 1.8  0.1
Additional systematics
Actual Rn activity
Air pockets likely small
Lateral diffusion (< 10 %)
Vacuum?
Humidity?
6 Conclusion
Method works reasonably well
  Potential to reduce systematics
    n production in PE not yet determined
7 Thanks
To my (summer) students:
Brian Drover,
Mina Rohanizadegan,
Graham Edge, Hai Jun Cho