## Slide 1: Low-background aspects of GERDA
Hardy Simgen
Max-Planck-Institut für Kernphysik / Heidelberg
on behalf of the GERDA collaboration

## Slide 2: Outline
Introduction
The GERDA experiment
Selected low-background aspects:
  Radio-purity of liquid argon
  Cryostat fabrication
  Frontend electronics radioactivity
  LAr scintillation veto
Conclusions

## Slide 3: The GERDA collaboration
~100 physicists
18 institutions
7 countries

## Slide 4: Double beta decay

## Slide 5: Double beta decay and Majorana neutrino mass
Phase space factor (~Qbb5)
Nuclear matrix element
Effective Majorana neutrino mass
If leading term is Majorana neutrino mass term
Coherent sum

## Slide 6: GERDA sensitivity
Feruglio, Strumia, Vissani NPB 659
phase II
phase I
KKDC claim
phase I
phase II
Using <M0n>=3.92, V.A. Rodin et al., Nucl. Phys. A 366 (2006) 107-131
Erratum: Nucl. Phys. A 793 (2007) 213-215
Assumes DE= 4 keV

## Slide 7: GERDA in brief
Ge spectroscopy with array of 76Ge-enriched diodes in ultrapure cryogenic liquid (LAr)
Phase I:
  Use of existing 76Ge-diodes from Heidelberg-Moscow and IGEX-experiments
  17.9 kg enriched diodes  ~15 kg 76Ge
  Bkg-level <10-2 counts/(keV·kg·y) @ 2039 keV to check KKCD-claim without background
Phase II:
  Adding new Ge diodes (total: ~40 kg 76Ge)
  New active background suppression techniques
  Demonstration of bkg-level <10-3 counts/(keV·kg·y) @ 2039 keV for a future one-ton experiment

## Slide 8: GERDA design
Cleanroom
Lock
Water tank (590 m3 H2O)
Cryostat (65 m3 LAr)

## Slide 9: GERDA design
Germanium-detector array
Vacuum-insulated double wall stainless steel cryostat
Additional inner copper shield
Liquid argon

## Slide 10
Cryostat delivery

## Slide 11
Water tank construction

## Slide 12
Installation of muon veto system

## Slide 14
Glove-box for Ge-detector handling under protective atmosphere

## Slide 16: Recent progress and status
December 2009: Liquid argon fill
January 2010: Commissioning of the cryogenic system
April/May 2010: Installation of the (commissioning-) lock
May 2010: 1st deployment of FE electronics & detector mock-up (27 pF)
  pulser resolution 1.4 keV (FWHM)
June 2010: First deployment of natGe detectors
Since July 2010: Commissioning run with natGe detector string (3 diodes):
1st data show more 42Ar than expected  requires dedicated analysis
Afterwards: Start phase I physics data taking

## Slide 17: GERDA phase II
37.8 kg of enrGe reduced and
purified (Yield: 35.5 kg 6N grade + 1.2 kg tail)
  Cosmic-ray exposure minimized
Baseline for phase II: Broad Energy Ge (BEGe) diodes (Fall-back: segmented diodes)
  Distinct pulse shapes  excellent
  multi-site event rejection
  LAr operation successfully tested
Entire BEGe production chain successfully tested with depGe

## Slide 18: Radio-purity of liquid argon
GERDA 222Rn specs: <0.5 μBq/m3 Ar (STP)
Cryo-adsorption of Rn on activated carbon proven to provide ultra-pure N2 (Borexino)
  Try to adapt same technique for LAr, but
    T(LAr) = T(LN2) + 10K
    Risk of Ar freezing
Tests performed using MoREx and low background proportional counters
  H. Simgen and G. Zuzel, Appl. Rad. Isot. 76 (2009) 922-925

## Slide 19: Results on 222Rn removal from Ar by cryo-adsorption
Gas phase results |  | 
Volume [liter LAr] | Reduction factor R | Leaking fract. 1/R [%]
96 | >360 | <0.28
169 | >1120 | <0.09
Liquid phase results |  | 
Volume [liter LAr] | Reduction factor R | Leaking fract. 1/R [%]
58 | 58.5  17.1 | 1.7  0.5
120 | 30.2  9.7 | 3.3  1.1
120 | 27.7  6.5 | 3.6  0.8
125 | 21.1  2.7 | 4.7  0.6
168 | 42.4  5.7 | 2.4  0.3
188 | 8.5  1.0 | 11.8  1.5
193 | 4.9  0.6 | 20.4  2.4
222 | 160  28 | 0.6  0.1
240 | 10.1  0.6 | 9.9  0.6

## Slide 20: Summary on Rn purification of Ar by cryo-adsorption
Gas phase purification very efficient
Liquid phase less efficient (poor kinetics)
Unclear picture, but factor 100 reduction seems possible with GERDA’s 1 kg carbon column
Problem: CarboAct activated carbon has very irregular shape:
  Not optimized for column purification
  Probably formation of accidental channels between carbon grains
  New product: Spherical carbon balls
    222Rn emanation: <0.5 mBq/kg

## Slide 21: 222Rn concentration in com- mercial Ar when truck is loaded
Company | Grade | 222Rn [mBq/m3 (STP)]
Air Liquide | technical (4.8) | 1.62  0.08
Air Liquide | technical (4.8) | 0.38  0.03
Westfalen AG | technical (4.6) | 1.11  0.05
Westfalen AG | technical (4.6) | 1.04  0.09
Westfalen AG | technical (4.6) | 0.50  0.02
Westfalen AG | technical (4.6) | 0.007  0.001
Westfalen AG | technical (5.0) | 8.4  0.4
Westfalen AG | high purity (6.0) | 0.38  0.01
LINDE | technical (5.0) | 0.37  0.06 *)
*) At time of delivery

## Slide 22: Initial Ar impurities
Ar is usually delivered from a local distribution center  Unknown storage time yields unpredictable results, because
  Initial 222Rn decays
  New 222Rn may be produced (emanation)
Trend shows higher initial 222Rn concentration in Ar than in N2 (~0.1 mBq/m3 (STP))
  Possible Explanation: Boiling points (Rn > Ar > N2)

## Slide 23: 222Rn emanation of storage tanks for cryogenic liquids
Tank from | Grade of stored gas | Vol. [m3] | 222Rn activity in saturation [mBq] | specific 222Rn act. [mBq/m3]
Westfalen AG | technical | 3 | 177  6 | 59  2
Air Liquide | technical | 0.67 | 1.8  0.4 | 2.7  0.6
LINDE | technical | 6.3 | 3.5  0.2 | 0.56  0.03
Westfalen AG | 6.0 | 0.67 | 42  2 | 63  3
SOL | 6.0 | 16 | 65  6 | 4.1  0.4
LINDE | 7.0 | 3 | 2.7  0.3 | 0.9  0.1

## Slide 24: 222Rn emanation of storage tanks for cryogenic liquids
Tank from | Grade of stored gas | Vol. [m3] | 222Rn activity in saturation [mBq] | specific 222Rn act. [mBq/m3]
Westfalen AG | technical | 3 | 177  6 | 59  2
Air Liquide | technical | 0.67 | 1.8  0.4 | 2.7  0.6
LINDE | technical | 6.3 | 3.5  0.2 | 0.56  0.03
Westfalen AG | 6.0 | 0.67 | 42  2 | 63  3
SOL | 6.0 | 16 | 65  6 | 4.1  0.4
LINDE | 7.0 | 3 | 2.7  0.3 | 0.9  0.1
Selected for GERDA

## Slide 25: The GERDA cryostat
Vacuum-insulated stainless-steel (SS) cryostat made from low-radioactivity austenitic steel
  228Th <1 mBq/kg for cylindrical part
  228Th <5 mBq/kg for top and bottom parts
  For all screening results see
  W. Maneschg et al., NIM A 593 (2008) 448–453
Additional passive copper shield inside
Active LN2 cooling system to avoid evaporation losses

## Slide 26: 222Rn emanation test of the GERDA cryostat
Remove air-borne 222Rn
Fill with 222Rn-free N2 (purified by cryo-adsorption)
Wait for ≥1 week to let grow-in emanating 222Rn
Mix to establish homogeneous 222Rn distribution
Extract small fraction of N2 from cryostat and determine its 222Rn concentration
Scale to entire cryostat to find total 222Rn emanation rate

## Slide 27: Cryostat 222Rn emanation
No. | Date | Description | Single results [mBq] | Average [mBq]
1 | Nov 07 | After construction and cleaning, no N2 mixing | 16.9  1.6stat  3.0sys 29.8  2.4stat  5.8sys | 23.3  3.6
2 | Mar 08 | After additional cleaning | 13.6  0.7stat  2.4sys 13.7  0.7stat  2.7sys | 13.7  1.9
3 | Jun 08 | After Cu mounting | 33.0  2.8stat  7.0sys 35.7  2.9stat  8.8sys | 34.4  6.0
4 | Nov 08 | After wiping of Cu / steel surfaces. | 33.2  3.5stat  1.9sys 31.3  4.6stat  3.4sys 27.3  2.4stat  0.7sys | 30.6  2.4
5 | Sep 09 | After mounting of shroud, manifold, compensator, and cryogenic tubing | 49.9  3.3stat  2.1sys 63.8  4.1stat  3.1sys 56.2  3.7stat  2.7sys 49.1  3.3stat  2.2sys | 54.7  3.5

## Slide 28: Radon shroud

## Slide 29: Welds as source for SS 222Rn emanantion
No | Description | Result [mBq/m]
1 | SS after welding | 0.36  0.04
2 | SS after welding + etching (HF+HNO3) | <0.1
3 | SS after welding + electropolishing | 0.10  0.04
4 | Sample No. 3 + additional etching | <0.04
Results on 222Rn emanation of welds
SS tape: (5 – 10) mBq/m2
  cannot explain cryostat result
Emanation of SS welds!
Surface effect: 226Ra can be removed by etching
Poster on surface cleaning from 222Rn daughters by G. Zuzel
What happens in LAr?  Next talk by Sebastian Lindemann

## Slide 30: Homogeneity test
Before mixing:
ctop = (0.42  0.05) mBq/m3 (STP)
cbot = (0.28  0.03) mBq/m3 (STP)
After mixing:
ctop = (0.23  0.03) mBq/m3 (STP)
cbot = (0.27  0.05) mBq/m3 (STP)
If system is untouched 222Rn is NOT homogeneously distributed
Relatively stronger 222Rn source in top part of cryostat

## Slide 31: Screening of GERDA FE electronics
Here I want to mention some results of the electronics screening, in particular the discovery of low 226Ra Ta capacitors and the purity of PEN cables.
Sample | 226Ra | 228Th | 228Ra | 40K
 | Units: mBq/piece |  |  | 
Old frontend „PZ0“ | 6.3  0.5 | 0.2  0.1 | 0.2  0.1 | 2.2  0.7
New frontend “CC2” | 0.32  0.09 | 0.44  0.10 | <0.36 | 2.6  1.3
Main source of 226Ra in PZ0: Ba containing capacitors |  |  |  | 
X5R capacitors (Ba) | 0.19  0.02 | 0.04  0.01 | <0.05 | <0.15
New capacitors (Ta) | <0.003 | 0.008  0.002 | <0.01 | 0.07  0.03
Improvements in CC2 with respect to PZ0:
  Number of components reduced
  Hot components removed (Ba capacitors, but also resistors, pins)
FE still critical for phase II background index
Paper in preparation

## Slide 34: Summary and conclusions
Many different techniques applied to control radiopurity of GERDA during construction
  LAr purity under control
  Cryostat emanation too high  shroud
  FE electronics critical, but OK for phase I
  Promising results from LAr scintillation veto (+ pusle shape discrimination with BEGe’s)
GERDA setup ready. Physics data taking will start after study of 42Ar issue