## Slide 1: Lead Removal from Liquid Scintillator for the Solar Phase of KamLAND
Greg Keefer
Lawrence Livermore National Lab
Aug. 28, 2010
LRT 2010, SNOLAB

## Slide 2: Low Energy Internal Backgrounds
 | T1/2 | Measured KamLAND Concentrations | Goal of Purification
210Pb | 22 y | (2.17 ± 0.09) x 10-20 g/g | 10-25 g/g
40K | 109 y | (1.3 ± 0.11) x 10-16 g/g | 10-18 g/g
39Ar | 269 y | < 4.3 x 10-21 g/g | 10-24 g/g
85Kr | 11 y | (6.10 ± 0.14) x 10-20 g/g | 10-26 g/g
238U | 109 y | (3.3 ± 0.5) x 10-18 g/g | 10-17 g/g
232Th | 1010 y | (5.2 ± 0.08) x 10-17 g/g | 10-16 g/g
10-25 g 210Pb /g LS → 400 210Pb atoms per m3 of LS!
The disequilibrium can be seen in the ratio of the T1/2
This is a result 222Rn contamination

## Slide 3: 210Pb Effect on the Low Energy Spectrum
KamLAND Integral Rate: 4 x 107 events/kton-day
BS05(OP) Expected Rate: 3 x 102 events/kton-day
250-800 keV

## Slide 4: How can one measure factors of 105 reduction in 210Pb at concentrations of 10-22 g/g in the LAB! ?

## Slide 5: Experimental Procedure
Fundamental Assumption:
All isotopes of Lead born via alpha decay will have similar chemical characteristics in liquid scintillator, or the individual components, and thus similar removal efficiencies in these liquids respectively.
We then use the 220Rn and 222Rn daughters from commercial sources (Pylon Electronics) to load 212Pb and 214Pb into the LS respectively.
At a concentration of 10-20 g/g the specific 212Pb activity is 0.83 Bq/l, a factor 1.8x104 larger than that of 210Pb at equal concentration.
Bubble LS with Rn loaded N2 gas and achieve activities on the order of 5 kBq/l depending on the liquid (LS, Dodecane, PC)

## Slide 6: Experimental Procedures Continued
Measure Gammas using Ge Detector:
  Specific activities down to 1 Bq/l
  Achieving 103 reduction
212/214Bi-Po b-a Coincidence
  Specific activities down to 10 mBq/l
  Achieving 105 orders of reduction capability
Thus, using these methods we can determine lead reduction in LS at the order of 105 and 212Pb concentrations as low as 10-17-10-22 g/g!

## Slide 7: How can one obtain factors of 105 reduction in 210Pb?

## Slide 8: Reducible Backgrounds
210Pb, 210Po, 210Bi, 222Rn
  Other contaminants to consider: 85Kr, 39Ar, 40K
I will present results from the in depth studies pertaining to the removal of radiogenic atoms and molecules from liquid scintillator via:
  Filtering
  HTiO
  Water Extraction
  Isotope Exchange, Filtering, HTiO
  Adsorption (SiO2, CuMn, Aerogels)
  Distillation
  Heating
  Chemical extraction

## Slide 9: Laboratory Results I
*note: Experiments performed on 212Pb unless specifically noted as using 214Pb.
Filtering:
  Observed that multiple passes through filters produced a factor 1.1 (10%) reduction in 212Pb
  Approximately factor 1.5 (30-40%) reduction was observed when the gas used to load the LS was not pre-filtered.
HTiO:
  0.64 g/cm3 HTiO was loaded on a HEPA PTFE filter. Then passed 125 ml LS at a rate of 3 and 16 cm3/min
  Observed small effect when passing through HTiO 1.06 ± 0.01

## Slide 10: Laboratory Results II
Lead Extraction with De-Ionized Water:
  Produced modest factors of 1.02 – 1.1 reduction in 212Pb
pH dependence with Water Extraction:
  Indicated a clear anti-correlation with pH (increased efficiency with lower pH)
  However, this was only a 15% increase relative to the DI Water.
Isotope Exchange:
  Pass the LS over bed of lead granules in hopes of an exchange of 210Pb for another isotope such as 206Pb. This would occur due
  No 212Pb reduction observed

## Slide 11: Laboratory Results III
Adsorption: removes charged atoms, i.e. Pb+2 or polar molecules by retention on the surfaces of the adsorption particles (silica gel, Alusil, Cu/Mn).
  212Pb: 89 ± 2 214Pb: 39 ± 8
  222Rn: 2.58 ± 0.01
  212Bi: > 633 214Bi: 79 ± 32
  214Pb: 39 ± 8
  218Po: 2.6 ± 0.5
Distillation:
  212Pb Reduction: 104 Measured by b-a coincidence of 212Bi – 212Po decay (0.43 ms)
  natKr Reduction: 105 Gas Chromatography
  222Rn Reduction: 106 Measured by b-a coincidence of 214Bi – 214Po decay (233 ms) *added small N2 flow
Tests our fundamental
hypothesis

## Slide 12
Radiation Interaction with Benzene Chains
n-dodecane
a decay
b decay
e- / e+ decay
nuclear recoil
Supplies sufficient kinetic energy to
break the C-C bond in molecule
Radioactive Tetramethyl lead
Most interactions create some ionic/polar species of the decay product.
However, ~5% of these atoms are bound in an organo-metallic compound

## Slide 13: Organic Pb Compounds
In order of decreasing molecular weight and increasing molecular stability.
Pb
Tetraethyllead C8H20Pb
BP: Decomposes at 200 oC
r: 1.653 g/cm3 @ 20 oC
Pb
Methyltriethyllead C7H18Pb
BP: 70 oC
r: 1.71 g/cm3 @ 20 oC
The fewer ethyl groups the lower the boiling point of the molecule.
Methyl Group
CH3
Ethyl Group
CH3CH2

## Slide 14
Pb
Ethyltrimethyllead C5H14Pb
BP: 27 oC
r: 1.88 g/cm3 @ 20 oC
Pb
Tetramethyllead C4H12Pb
BP: 110 oC
r: 1.995 g/cm3 @ 20 oC
Pb
Diethyldimethyllead C6H16Pb
BP: 51 oC
r: 1.79 g/cm3 @ 20 oC
Organic Pb Compounds

## Slide 15: Laboratory Results IV
Heating: Used to break organo-metallic bonds, which then ionize the Pb, Po, Bi, etc. atom and can be removed by adsorption or distillation.
  Operating Temperature: 100 – 200 oC
  Used in combination with adsorption column
    212Pb Reduction boost factor: 10 (Total 212Pb reduction = 278 ± 23)
FeCl3 SnCl4 MoS2 and Thiol Resin:
  SiO2 + FeCl3 + SiO2: 1250
  However, these are very destructive to the LS.

## Slide 16: Results of Laboratory Experiments
Distillation was the best purification method for removing metallic radio-isotopes
  104 reduction in 212Pb observed
  This method is extremely tedious and care must be taken:
    remove the first and last amounts of liquid
    Never allow to rapidly boil, smooth processes
    Multiple distillation > 3x to achieve 104
Observed of an organic component of 212/214Pb (using Silica Gels)
  Evidence of existence by performing experiments to address this specific species resulted in high removal efficiencies.
  Must be addressed to achieve ultra-pure liquid scintillator.

## Slide 17: Backgrounds from Calibration Deployments
Not controlling backgrounds during calibration can re-contaminate your experiment with 210Pb:
Observed: 0.13-8.0 mBq 210Pb / deployment
Requirement: < 1 mBq 210Pb or contaminations < mBq/m3 222Rn
Berger,B. et al., JINST 4:P04017,2009

## Slide 18: References of Interest
Preparing NIM paper on the removal of Radon Daughters from KamLAND LS.
  My thesis provides extensive details on these measurements and is the basis for the NIM paper. Can be found on SPIRES
  There are also colleagues from Tohoku University who performed complementary studies and wrote Masters thesis. However, only available in Japanese.
The Silica Gels were counted for radio-purity on HPGe to determine Rn out-gassing and other possible contamination. These can be found in the EXO publication mentioned by Ryan MacLellan.
  D.S. Leonard et al., Nucl.Instrum.Meth.A591:490-509,2008

## Slide 19: Questions ??
Heating
Water Extraction
Adsorbents
Distillation

## Slide 20: Supplemental Slides

## Slide 21: Properties of the Solvent
n-dodecane should be considered the solvent since it is the
dominant molecule and is non-polar.
CH3-(CH2)10-CH3
BP: 215-217 oC @ 760.00 mmHg
MP: -9.6 oC
r: 0.7495 g/cm3 @ 20 oC
Interacts with the other molecules by dispersive forces,
a statistically random induced dipole moment.
All values on this and the next slides were obtained from the CRC.

## Slide 22: What Solutes are in KamLAND?
1,2,4-Trimethybenzene (PC)
CH3
CH3
CH3
C6H3(CH3)3
BP: 169 oC @ 760.00 mmHg
MP: -43.77 oC
r: 0.8758 g/cm3 @ 20 oC
2,5 Diphenyloxazole (PPO)
N
O
C15H11NO
BP: 360 oC @ 760.00 mmHg
MP: 74 oC
r: 1.0940 g/cm3 @ 20 oC
Chromatographic separation at the MP of PPO may allow us to reduce
The amount of PPO adsorbed onto the surface of the Silica Gel.
PC and PPO are
Aromatic Molecules

## Slide 23: Some Interesting Data for Dodecane
N-dodecane from Aldrich Chem. Co. was purified with active alumina
and silica gel column, then distilled. > 99.2% pure n-dodecane.
The dodecane was doped with up to 10 mM of different aromatic
hydrocarbons.
The samples were then exposed to 100 kGy = 100 kJ/kg of 60Co gamma
rays.
- They then analyzed the samples for fragmented molecules.
Result:
The larger the concentration of aromatic molecules
in the dodecane the lower the concentration of
fragmented C-chains after irradiation.

## Slide 24: KamLAND Detector Details
1325 17 inch PMTs
554 20 inch PMTs
photocathode coverage:
22% (17 inch)
34% (17+20 inch)
Filled with mineral oil
0.9 ktons Liquid Scintillator
80.2% n-Dodecane
19.8% Pseudocumene
1.36 g/L PPO (primary fluor)
Balloon 135 mm (Nylon/EVOH)
13 m diameter
Kavlar ropes
Non-scintillating buffer region
(1.4 ktons mineral oil)
Calibration system
(z-axis and 4pi systems)
Water Cherenkov
Outer detector
(2.6 ktons)
Acrylic sphere to shield from 222Rn out-gassing from the PMTs and SS sphere
225 20 inch PMTs
Stainless steel containment vessel (18 m diameter)

## Slide 25: Integrated Regions 250 – 800 keV
Solar ne Elastic Scattering | Rate [Events/kton-day]
13N | 13.7
15O | 15.8
17F | 0.4
(862 keV) 7Be | 290.8
(384 keV) 7Be | 0.5
8B | 0.5
PEP | 13.4
PP | 12.2
Total Solar Signal | 347
Radio-isotope | Rate [Events/kton-day]
40K | 21.6
85Kr | 37.6
39Ar | 0.1
210Bi | 29.1
210Po | 30.7
11C | 0.5
238U | 2.0
232Th | 13.1
Total Background | 135
Expected Signal-to-background ratio: 2.6